七篇 DoubleSAM / Co-SAM 文献电学表征分类及原文汇总

1. 电流密度–电压特性与光伏参数（J–V / Photovoltaic parameters）

Poly-SAM（PDF 第 5 页）

Original: Employing PTP-SAM to minimize current leakage at the buried interface led to an increase in average PCE from 25.7% to 26.1% (Supplementary Fig. 43), primarily due to improvements in the fill factor (FF) and open-circuit voltage (VOC), which can be attributed to enhanced shunt resistance, favourable band alignment and reduced recombination at the buried interface (Fig. 3b and Supplementary Figs. 44 and 45).

中文：采用 PTP-SAM 最小化埋底界面的漏电流，使平均 PCE 从 25.7% 提高到 26.1%（补充图 43），这主要归因于填充因子（FF）和开路电压（VOC）的改善，可归因于增强的并联电阻、有利的能带对齐以及埋底界面处复合的减少（图 3b 和补充图 44 与 45）。

Poly-SAM（PDF 第 6 页）

Original: The best-performing target device with a PTP-SAM layer showed a maximum PCE of 26.3% with a VOC of 1.185 V, FF of 85.1% and short-circuit current density (JSC) of 26.11 mA cm−2, while a control device with a SAM layer showed a maximum PCE of 25.9% with a VOC of 1.177 V, FF of 84.2% and JSC of 26.16 mA cm−2 (Fig. 3c).

中文：具有 PTP-SAM 层的最佳目标器件表现出 26.3% 的最高 PCE，VOC 为 1.185 V，FF 为 85.1%，短路电流密度（JSC）为 26.11 mA cm−2，而具有 SAM 层的对照器件最高 PCE 为 25.9%，VOC 为 1.177 V，FF 为 84.2%，JSC 为 26.16 mA cm−2（图 3c）。

Poly-SAM（PDF 第 8 页）

Original: The best-performing target PSM achieved a PCE of 24.0%, with a VOC of 9.50 V, FF of 82.0% and JSC of 3.08 mA cm−2. For comparison, the control PSM exhibited a VOC of 9.41 V and FF of 77.5%, corresponding to a PCE of 22.5% (Fig. 4d).

中文：最佳性能的目标 PSM 实现了 24.0% 的 PCE，VOC 为 9.50 V，FF 为 82.0%，JSC 为 3.08 mA cm−2。作为比较，对照 PSM 表现出 9.41 V 的 VOC 和 77.5% 的 FF，对应 22.5% 的 PCE（图 4d）。

Poly-SAM（PDF 第 8 页）

Original: One target PSM was sent to the National Photovoltaic Industry Metrology Test Center (NPVM) for certification, which confirmed a reverse-scan PCE of 23.4% and a stabilized MPPT efficiency of 23.2% with the highest VOC × FF (Fig. 4e and Supplementary Figs. 52 and 53). This certified value marks the first reported steady-state PCE to surpass 23% at the module level and has been included in the solar cell efficiency tables in ref. 34 (Fig. 4f and Supplementary Table 1).

中文：一个目标 PSM 被送往国家光伏产业计量测试中心（NPVM）进行认证，确认其反向扫描 PCE 为 23.4%、稳定 MPPT 效率为 23.2%，并具有最高的 VOC × FF（图 4e 和补充图 52 与 53）。该认证值标志着首个在组件级别超过 23% 的稳态 PCE 报道，并已被收录于参考文献 34 的太阳能电池效率表中（图 4f 和补充表 1）。

Poly-SAM（PDF 第 8 页）

Original: J–V measurements of the devices were performed with a Keithley 2400 source meter under simulated 1-sun AM1.5G illumination (100 mW cm−2) using an ABET Technologies Sun 2000 solar simulator. The measurements were performed in an N2-filled glove box. The illumination area of the devices was defined by shadow masks with areas of 0.05 and 20.25 cm2.

中文：器件的 J–V 测量使用 Keithley 2400 源表，在模拟 1 个太阳 AM1.5G 光照（100 mW cm−2）下、采用 ABET Technologies Sun 2000 太阳模拟器进行。测量在充氮手套箱中进行。器件的照射面积由面积为 0.05 和 20.25 cm2 的阴影掩模限定。

DoubleSAM 2PACz Me-4PACz（PDF 第 6 页）

Original: The control cell yielded a champion PCE of 18.76% (18.49%) with a VOC of 1.33 V (1.33 V), short-circuit current density (JSC) of 17.54 mA cm2 (17.47 mA cm2), and FF of 80.63% (79.80%) under reverse (forward) scan.

中文：对照组电池在反向（正向）扫描下获得 18.76%（18.49%）的冠军 PCE，VOC 为 1.33 V（1.33 V），短路电流密度（JSC）为 17.54 mA cm−2（17.47 mA cm−2），FF 为 80.63%（79.80%）。

DoubleSAM 2PACz Me-4PACz（PDF 第 6 页）

Original: By contrast, the target cell delivered a champion PCE of 19.83% (19.67%), with a VOC of 1.35 V (1.35 V), JSC of 17.65 mA cm2 (17.62 mA cm2) and FF of 83.11% (82.64%) under reverse (forward) scan.

中文：相比之下，目标电池在反向（正向）扫描下获得了 19.83%（19.67%）的冠军 PCE，VOC 为 1.35 V（1.35 V），JSC 为 17.65 mA cm−2（17.62 mA cm−2），FF 为 83.11%（82.64%）。

DoubleSAM 2PACz Me-4PACz（PDF 第 6 页）

Original: The statistical distribution of device metrics is presented in Fig. 4b and Fig. S18 (ESI†). Notably, compared to the control ones, the target cells exhibit significant improvements in VOC and FF, resulting in higher average PCE.

中文：器件指标的统计分布见图 4b 和图 S18（ESI†）。值得注意的是，与对照组相比，目标电池在 VOC 和 FF 方面表现出显著提升，从而获得了更高的平均 PCE。

DoubleSAM 2PACz Me-4PACz（PDF 第 6 页）

Original: Furthermore, we achieved a champion VOC of 1.36 V, which represents one of the highest VOC values and lowest VOC-deficit value reported for WBG (1.75–1.85 eV) perovskite solar cells (Fig. 4d and Fig. S19–S21, Table S2, ESI†).

中文：此外，我们实现了 1.36 V 的冠军 VOC，这是已报道的 WBG（1.75–1.85 eV）钙钛矿太阳能电池中最高的 VOC 值和最低的 VOC 亏损值之一（图 4d 及图 S19–S21、表 S2，ESI†）。

DoubleSAM 2PACz Me-4PACz（PDF 第 7 页）

Original: We also applied the method to other WBG perovskite compositions like 1.66 eV FA0.8Cs0.2Pb(I0.8Br0.2)3, which is suitable for perovskite/silicon tandem solar cells. The obtained results (Fig. S25, ESI†) exhibit similar trends, indicating the universality of the Me-4PACz interface engineering strategy.

中文：我们还将该方法应用于其他 WBG 钙钛矿组分，例如适用于钙钛矿/硅叠层太阳能电池的 1.66 eV FA0.8Cs0.2Pb(I0.8Br0.2)3。所获得的结果（图 S25，ESI†）表现出相似的趋势，表明 Me-4PACz 界面工程策略具有普适性。

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: The I–V curves for the devices with different substrates are shown in Figure 4b and the device using Me-4PACz as the hole-selective layer obtained a PCE of 22.87% with the Voc, short-circuit current density (Jsc) and FF of 1.13 V, 24.92 mA cm−2 and 81.21% under reverse scan, respectively.

中文：不同基底器件的I–V曲线如图4b所示，以Me-4PACz作为空穴选择层的器件在反向扫描下获得的PCE为22.87%，其Voc、短路电流密度（Jsc）和FF分别为1.13 V、24.92 mA cm−2和81.21%。

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: In comparison, the device with an optimal concentration of 0.2 mg ml−1 (Figure S19 and Table S3, Supporting Information) obtained a PCE of 25.16% with the Voc, Jsc and FF of 1.20 V, 25.10 mA cm−2 and 83.54%, respectively, under reverse scan.

中文：相比之下，采用最佳浓度0.2 mg ml−1的器件（图S19和表S3，支持信息）在反向扫描下获得的PCE为25.16%，其Voc、Jsc和FF分别为1.20 V、25.10 mA cm−2和83.54%。

DoubleSAM Me-4PACz Br-EPA（PDF 第 5 页）

Original: One of the devices based on BEpo-SAM is sent to an accredited independent PV test laboratory (Shanghai Institute of Microsystem and Information Technology (SIMIT), Shanghai, China) for certification and a PCE of 24.67% under forward scan and 24.61% under reverse scan was certified (Figure S20, Supporting Information) with negligible hysteresis.

中文：其中一个基于BEpo-SAM的器件被送往经认可的独立光伏测试实验室（中国上海，中国科学院上海微系统与信息技术研究所（SIMIT））进行认证，认证结果为正向扫描下PCE为24.67%、反向扫描下为24.61%（图S20，支持信息），迟滞可忽略。

DoubleSAM2（PDF 第 9 页）

Original: Consequently, the BL-SAM device achieved a champion PCE of 20.35% with an exceptional FF of 85.18%, representing state-of-the-art performance for 1.79 eV WBG PSCs. Additionally, this strategy proved to be equally applicable to devices with a bandgap of 1.85 eV, yielding a champion PCE of 19.24% with VOC of 1.39 V.

中文：因此，BL-SAM器件实现了20.35%的冠军PCE和85.18%的优异FF，代表了1.79 eV WBG PSC的最新水平。此外，该策略同样适用于带隙为1.85 eV的器件，获得了19.24%的冠军PCE和1.39 V的VOC。

DoubleSAM2（PDF 第 10 页）

Original: The current density-voltage (J–V) characteristics of the photovoltaic devices were measured at room temperature within a nitrogen-filled glovebox, employing a xenon lamp solar simulator (Enlitech, SS-X50, Taiwan). The illumination intensity was calibrated to 100 mW cm−2 using a silicon reference cell equipped with a KG2 filter. Device performance was evaluated using an IVS-KA6000 source meter under both reverse (1.35 to −0.1 V) and forward (−0.1 to 1.35 V) scanning modes, with a scan rate of 0.01 V s−1 and a delay time of 10 ms. The active area for all devices was defined as 0.06 cm2 by a metal mask, and no preconditioning procedures were applied prior to testing.

中文：光伏器件的电流密度-电压（J–V）特性在氮气填充手套箱内于室温下测量，使用氙灯太阳光模拟器（Enlitech, SS-X50, 台湾）。光照强度使用配备KG2滤光片的硅参比电池校准至100 mW cm−2。器件性能使用IVS-KA6000源表在反扫（1.35至−0.1 V）和正扫（−0.1至1.35 V）两种扫描模式下评估，扫描速率为0.01 V s−1，延迟时间为10 ms。所有器件的有效面积由金属掩模限定为0.06 cm2，测试前未施加任何预处理程序。

DoubleSAM3（PDF 第 4 页）

Original: To investigate the influence of different HTLs on device performance, we fabricated the wide-bandgap (1.68 eV) PPVs with the structure ITO/HTL/perovskite/C60/SnO2/Ag (Figure 3a). Figure 3b shows the current density−voltage (J−V) curves of devices with the corresponding photovoltaic parameters of the champion devices (Table S4). The results indicate that devices employing CbzBF, CbzBT, and CbzBF/CbzBT all exhibit significantly improved photovoltaic performance compared to the MeO-4PACz-based devices. The champion device is prepared with CbzBF/CbzBT bilayer,

中文：为研究不同 HTL 对器件性能的影响，我们制备了结构为 ITO/HTL/perovskite/C60/SnO2/Ag 的宽禁带（1.68 eV）PPV（图 3a）。图 3b 展示了器件的电流密度–电压（J−V）曲线及相应冠军器件的光伏参数（Table S4）。结果表明，采用 CbzBF、CbzBT 和 CbzBF/CbzBT 的器件相比基于 MeO-4PACz 的器件均表现出显著改善的光伏性能。冠军器件采用 CbzBF/CbzBT 双层制备，

DoubleSAM3（PDF 第 5 页）

Original: To validate the universality of CbzBF/CbzBT bilayer as a hole transport layer, we conducted a comprehensive performance comparison with MeO-4PACz, CbzBF, and CbzBT in PPVs with bandgaps of 1.65, 1.72, and 1.75 eV (Figure S8). Figures S9 and S10 indicate best ratio of CbzBF/CbzBT bilayer is 1:1. The J−V characteristics (Figure S11), EQE spectra (Figure S12), and champion device parameters (Tables S5−S7) consistently demonstrate that the CbzBF/CbzBT bilayer structure delivers optimal performance across all bandgap systems. Notably, high FFs of 85.65, 85.99, and 85.03% are achieved in 1.65, 1.72, and 1.75 eV perovskite,

中文：为验证 CbzBF/CbzBT 双层作为空穴传输层的普适性，我们在带隙为 1.65、1.72 和 1.75 eV 的 PPV 中与 MeO-4PACz、CbzBF 和 CbzBT 进行了全面的性能比较（图 S8）。图 S9 和 S10 表明 CbzBF/CbzBT 双层的最佳比例为 1:1。J−V 特性（图 S11）、EQE 光谱（图 S12）和冠军器件参数（Tables S5−S7）一致表明，CbzBF/CbzBT 双层结构在所有带隙体系中均提供最佳性能。值得注意的是，在 1.65、1.72 和 1.75 eV 钙钛矿中分别获得了 85.65、85.99 和 85.03% 的高 FF，

DoubleSAM3（PDF 第 6 页）

Original: respectively. Furthermore, we fabricated 20 independent devices for each bandgap (1.65, 1.68, 1.72, and 1.75 eV) and performed systematic statistical analysis of JSC, VOC, FF, and PCE (Figures 3g,h and S13). The results consistently confirm that the sequential deposition strategy of CbzBF/CbzBT markedly enhances device performance and reproducibility.

中文：分别为相应数值。此外，我们针对每种带隙（1.65、1.68、1.72 和 1.75 eV）制备了 20 个独立器件，并对 JSC、VOC、FF 和 PCE 进行了系统的统计分析（图 3g,h 和 S13）。结果一致证实，CbzBF/CbzBT 的顺序沉积策略显著提升了器件性能和可重复性。

DoubleSAM3（PDF 第 6 页）

Original: Finally, by comparing the FF values obtained in this work with recently reported data for 1.65−1.75 eV single-junction perovskite cells (Figure 3i), we observed that devices with CbzBF/CbzBT bilayer achieve high FFs within the highest reported range in the literature.

中文：最后，通过将本工作获得的 FF 值与近期报道的 1.65−1.75 eV 单结钙钛矿电池数据进行比较（图 3i），我们观察到采用 CbzBF/CbzBT 双层的器件实现了处于文献报道最高范围内的高 FF。

DoubleSAM3（PDF 第 6 页）

Original: Then, we evaluate the performance of wide-bandgap PPVs for indoor photovoltaic (LED, 1000 lx, 301.9 μW·cm−2) applications. As shown in Figures 4a,b and S14, compared to the MeO-4PACz-based PPVs, CbzBF, CbzBT, and the CbzBF/CbzBT bilayer HTL deliver significant improvements in both VOC and JSC, leading to a notable enhancement in average PCE. The J−V characteristics and champion device parameters are summarized in Figure 4e and Table S9, respectively. Notably, PCEs of 41.92, 43.88, 43.19, and 42.12% were achieved in perovskite devices with bandgaps of 1.65, 1.68, 1.72, and 1.75 eV. Corresponding high VOC of 1.031, 1.07, 1.083, and 1.083 V were also obtained, further affirming the superior performance enabled by the sequential deposition of the CbzBF/CbzBT bilayer.

中文：随后，我们评估了宽禁带 PPV 在室内光伏（LED，1000 lx，301.9 μW·cm−2）应用中的性能。如图 4a,b 和 S14 所示，与基于 MeO-4PACz 的 PPV 相比，CbzBF、CbzBT 和 CbzBF/CbzBT 双层 HTL 在 VOC 和 JSC 上均带来显著提升，从而使平均 PCE 明显增强。J−V 特性和冠军器件参数分别总结于图 4e 和 Table S9。值得注意的是，带隙为 1.65、1.68、1.72 和 1.75 eV 的钙钛矿器件分别获得了 41.92、43.88、43.19 和 42.12% 的 PCE。还获得了相应的高 VOC，分别为 1.031、1.07、1.083 和 1.083 V，进一步证实了 CbzBF/CbzBT 双层顺序沉积所带来的优越性能。

DoubleSAM-SAME（PDF 第 8 页）

Original: As shown in Figure 5b, the control devices with unwashed MeO-2PACz achieved a maximum power conversion efficiency (PCE) of 21.7% (22.0% under reverse scanning), which increased to 22.1% (22.3% under reverse scanning) after redepositionthe highest PCE observed among all processing conditions tested (Figure S60 and Table S8).

中文：如图5b所示，使用未清洗MeO-2PACz的对照器件实现了21.7%的最大功率转换效率（PCE）（反向扫描下为22.0%），在重新沉积后提高到22.1%（反向扫描下为22.3%），这是所有测试的加工条件中观察到的最高PCE（图S60和表S8）。

DoubleSAM-SAME2（PDF 第 5 页）

Original: In contrast, the optimized D-2P-treated PSC achieved a champion PCE of 20.80% (Supplementary Fig. 25, Supplementary Table 1). And a certified PCE of 20.7% was obtained at SIMIT (Fig. 4b, Supplementary Fig. 26), which is the highest value reported for a WBG PSC with a bandgap wider than 1.74 eV (Fig. 4c, Supplementary Table 2).

中文：相比之下，优化后的 D-2P 处理 PSC 实现了 20.80% 的冠军 PCE（补充图 25，补充表 1）。并且在 SIMIT 获得了 20.7% 的认证 PCE（图 4b，补充图 26），这是带隙宽于 1.74 eV 的 WBG PSC 报道的最高值（图 4c，补充表 2）。

DoubleSAM-SAME2（PDF 第 7 页）

Original: To show the application potential of WBG PSCs with D-2P structure, we fabricated a semitransparent device to construct four-terminal (4-T) all-perovskite tandem solar cell with NBG perovskite bottom cell (Fig. 4g). The resulting semitransparent WBG PSC yielded a PCE of 19.35% with a Voc of 1.30 V. The filtered NBG PSC possessed a PCE of 8.73% based on an initial PCE of 21.70% (Fig. 4h and Supplementary Table 7).

中文：为了展示具有 D-2P 结构的 WBG PSC 的应用潜力，我们制备了半透明器件，以构建带有 NBG 钙钛矿底电池的四端（4-T）全钙钛矿叠层太阳能电池（图 4g）。所得的半透明 WBG PSC 产生了 19.35% 的 PCE，Voc 为 1.30 V。经过滤的 NBG PSC 在初始 PCE 为 21.70% 的基础上具有 8.73% 的 PCE（图 4h 和补充表 7）。

DoubleSAM-SAME2（PDF 第 7 页）

Original: The reduced PCE of the filtered NBG PSC is mainly ascribed to the sharp decline in Jsc from 31.52 to 12.87 mA cm−2, which is in accordance with the corresponding EQE spectra (Fig. 4i).

中文：经过滤的 NBG PSC 的 PCE 降低主要归因于 Jsc 从 31.52 急剧下降到 12.87 mA cm−2，这与相应的 EQE 光谱一致（图 4i）。

DoubleSAM-SAME2（PDF 第 9 页）

Original: As a result, D-2P-treated PSC (1.75 eV) achieved a champion PCE of 20.80% (certified 20.70%), which is the highest value reported for a WBG PSC with a bandgap wider than 1.74 eV.

中文：结果，D-2P 处理的 PSC（1.75 eV）实现了 20.80% 的冠军 PCE（认证值 20.70%），这是带隙宽于 1.74 eV 的 WBG PSC 报道的最高值。

DoubleSAM-SAME2（PDF 第 9 页）

Original: The Voc and Jsc were measured using a Keithley 2400 instrument. Instantaneous J-V curves then measured with a scanning rate of 100 mV s−1 (voltage step of 20 mV and delay time of 200 ms). The devices were measured by a customized mask with an effective area of 0.089 cm−2. The output of the light source was adjusted using a calibrated silicon photodiode (Newport) at 1 sun (100 mW cm−2). The J-V curves is measured in atmospheric conditions. Through the silicon standard cells (SRC-00288, Enli Tech) and sun simulator (SS-F5, Enli Tech) for light intensity calibration.

中文：Voc 和 Jsc 使用 Keithley 2400 仪器测量。随后以 100 mV s−1 的扫描速率测量瞬时 J-V 曲线（电压步长 20 mV，延迟时间 200 ms）。器件使用有效面积为 0.089 cm−2 的定制掩模进行测量。光源输出使用经校准的硅光电二极管（Newport）在 1 个太阳（100 mW cm−2）下调节。J-V 曲线在大气条件下测量。通过硅标准电池（SRC-00288，Enli Tech）和太阳模拟器（SS-F5，Enli Tech）进行光强校准。

2. 迟滞与扫描速率依赖（Hysteresis / Scan-rate dependence）

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: The significant improvement in Voc and FF and reduced hysteresis factor Hi from 1.5% to 0.8% (Table S4, Supporting Information) can be mainly attributed to the more compact po-SAM with less voids and the passivation effect of Br-EPA at the buried interface.

中文：Voc和FF的显著提升以及迟滞因子Hi从1.5%降低到0.8%（表S4，支持信息），主要归因于更致密、空洞更少的po-SAM以及Br-EPA在埋底界面的钝化作用。

DoubleSAM2（PDF 第 10 页）

Original: under both reverse (1.35 to −0.1 V) and forward (−0.1 to 1.35 V) scanning modes, with a scan rate of 0.01 V s−1 and a delay time of 10 ms.

中文：在反扫（1.35至−0.1 V）和正扫（−0.1至1.35 V）两种扫描模式下，扫描速率为0.01 V s−1，延迟时间为10 ms。

3. 暗电流、反向偏压与击穿特性（Dark current / Reverse bias / Breakdown）

Poly-SAM（PDF 第 5 页）

Original: Furthermore, we employed lock-in thermography to assess the enhanced robustness and compactness of the buried interface over a large area. SAM- and PTP-SAM-based solar modules with an area of 20 cm2 were biased at the negative voltage at the maximum power point (−VMPP, where VMPP = 8.1 V) in air to monitor increases in temperature under reverse bias. In the SAM-based device, hot spots appeared within seconds of reverse biasing, indicating reverse current flow and localized Joule heating (Fig. 2j and Supplementary Fig. 41a–c). The average temperature in some regions increased by 5 °C within 25 s (Supplementary Fig. 42a,b). In contrast, no hot spots were observed in the PTP-SAM-based device, even after applying a bias for 5 min (Fig. 2k and Supplementary Fig. 41d–f), and the temperature across the whole device remained largely unchanged (Supplementary Fig. 42c,d).

中文：此外，我们采用锁相热成像来评估大面积埋底界面增强的稳健性和致密性。面积为 20 cm2 的基于 SAM 和 PTP-SAM 的太阳能组件在空气中被偏置到最大功率点处的负电压（−VMPP，其中 VMPP = 8.1 V），以监测反向偏压下的温升。在基于 SAM 的器件中，反向偏置后数秒内就出现了热点，表明存在反向电流流动和局部焦耳加热（图 2j 和补充图 41a–c）。某些区域的平均温度在 25 s 内升高了 5 °C（补充图 42a,b）。相比之下，在基于 PTP-SAM 的器件中，即使施加偏压 5 min 也未观察到热点（图 2k 和补充图 41d–f），整个器件的温度基本保持不变（补充图 42c,d）。

Poly-SAM（PDF 第 7 页）

Original: The target devices maintained a consistently low reverse current when increasing the reverse bias up to −5.0 V, indicating a strong electron-blocking capability at the buried interface (Fig. 3f and Supplementary Fig. 48), whereas the SAM-based devices showed a sharp increase in current when the reverse bias was increased beyond −2.5 V.

中文：目标器件在反向偏压增大到 −5.0 V 时始终保持低反向电流，表明埋底界面具有很强的电子阻挡能力（图 3f 和补充图 48），而基于 SAM 的器件在反向偏压超出 −2.5 V 时电流急剧增加。

Poly-SAM（PDF 第 9 页）

Original: For lock-in thermography, in situ thermal imaging was conducted using a FLIR A655sc infrared camera, primarily operating at frame rates between 1 and 5 Hz, depending on the measurement conditions. A programmable DC source (SourceMeter) was used to apply controlled forward and reverse biases to the devices. Reverse-bias experiments were performed predominantly under −8.1 V. During measurements, no external illumination was applied and the experiments were carried out under ambient air conditions with temperatures between 22 and 24 °C.

中文：对于锁相热成像，使用 FLIR A655sc 红外相机进行原位热成像，主要工作帧率为 1 至 5 Hz，具体取决于测量条件。使用可编程直流电源（SourceMeter）向器件施加受控的正向和反向偏压。反向偏压实验主要在 −8.1 V 下进行。测量期间不施加外部光照，实验在环境空气条件下、温度介于 22 至 24 °C 之间进行。

DoubleSAM Me-4PACz Br-EPA（PDF 第 5 页）

Original: In conclusion, a po-SAM strategy is proposed and realized by the post-assembled Br-EPA to fill the voids of Me-4PACz, which forms a densely packed monolayer with minimal voids to reduce the current leakage of the devices.

中文：总之，本文提出并实现了通过后组装Br-EPA填充Me-4PACz空洞的po-SAM策略，形成了空洞极少的致密堆积单分子层，从而降低器件的电流泄漏。

4. 外量子效率与电致发光（EQE / EQEEL / EL）

Poly-SAM（PDF 第 6 页）

Original: The integrated JSC of the target device was calculated to be 25.7 mA cm−2 from the external quantum efficiency (EQE), which is consistent with the J–V curves (Supplementary Fig. 46).

中文：根据外量子效率（EQE）计算得到目标器件的积分 JSC 为 25.7 mA cm−2，与 J–V 曲线一致（补充图 46）。

Poly-SAM（PDF 第 9 页）

Original: EQE measurements were conducted using a Bentham PVE300-IVT system. The LED laser intensity was calibrated using built-in silicon and germanium diodes before measurements. For high-resolution EQE measurements, the light was chopped at 137 Hz and coupled to a Bentham monochromator. The resulting monochromatic light was focused on the perovskite solar cell and its current under short-circuit conditions was fed to a current pre-amplifier (Stanford SR 570) before analysis with a lock-in amplifier (Stanford SR830 DSP). The time constant of the lock-in amplifier was chosen to be 1 s and the amplification of the pre-amplifier was increased to resolve low photocurrents. EQEs were calculated by dividing the photocurrent of the cell by the flux of incoming photons, which was measured using a calibrated Si photodiode. All EQE measurements were performed under ambient conditions at 25 °C with a RH of around 60% and without encapsulation.

中文：EQE 测量使用 Bentham PVE300-IVT 系统进行。测量前使用内置硅和锗二极管对 LED 激光强度进行校准。对于高分辨率 EQE 测量，光以 137 Hz 斩波并耦合到 Bentham 单色仪。所得单色光聚焦在钙钛矿太阳能电池上，其在短路条件下的电流被送入电流前置放大器（Stanford SR 570），然后用锁相放大器（Stanford SR830 DSP）进行分析。锁相放大器的时间常数选择为 1 s，并提高前置放大器的放大倍数以分辨低光电流。EQE 通过将电池的光电流除以入射光子通量计算得到，入射光子通量使用校准的 Si 光电二极管测量。所有 EQE 测量均在 25 °C、RH 约 60% 的环境条件下、无封装情况下进行。

DoubleSAM 2PACz Me-4PACz（PDF 第 6 页）

Original: External quantum efficiency (EQE) of the champion cells is illustrated in Fig. 4c. The target cell demonstrated higher EQE values and integral JSC than the control one, consistent with the J–V scan results.

中文：冠军电池的外量子效率（EQE）如图 4c 所示。目标电池表现出比对照组更高的 EQE 值和积分 JSC，与 J–V 扫描结果一致。

DoubleSAM 2PACz Me-4PACz（PDF 第 7 页）

Original: The integrated JSC values obtained from EQE spectra for the WBG and NBG sub-cells are 16.0 and 15.5 mA cm2, respectively, which are in good agreement with the JSC values determined from J–V measurements (Fig. 5c).

中文：由 EQE 谱得到的 WBG 和 NBG 子电池的积分 JSC 分别为 16.0 和 15.5 mA cm−2，这与由 J–V 测量确定的 JSC 值吻合良好（图 5c）。

DoubleSAM Me-4PACz Br-EPA（PDF 第 5 页）

Original: The external quantum efficiency (EQE) curves for the control and the target devices are displayed in Figure 4c for Jsc calibration. The integrated Jsc of the devices based on Me-4PACz and BEpo-SAM are 24.86 and 25.35 mA cm−2, respectively, which match well with the observed Jsc in I–V curves. The increase in the quantum efficiency can be attributed to the improved perovskite crystallization.

中文：对照器件和目标器件的外量子效率（EQE）曲线如图4c所示，用于Jsc校准。基于Me-4PACz和BEpo-SAM的器件的积分Jsc分别为24.86和25.35 mA cm−2，与I–V曲线中观测到的Jsc吻合良好。量子效率的提高可归因于钙钛矿结晶的改善。

DoubleSAM3（PDF 第 5 页）

Original: The external quantum efficiency (EQE) spectra of the champion devices with the four HTLs are presented in Figure 3c. All the integrated current densities are consistent with the J−V measurement results.

中文：四种 HTL 的冠军器件的外量子效率（EQE）光谱见图 3c。所有积分电流密度均与 J−V 测量结果一致。

DoubleSAM3（PDF 第 7 页）

Original: External quantum efficiency (EQE) spectra were obtained using an Enlitech QE-R system calibrated with a certified silicon reference cell. For two-terminal perovskite/silicon tandem solar cells, the EQE of the silicon bottom subcell was measured using a 500 nm short-pass optical filter, while that of the perovskite top subcell was measured using an 850 nm long-pass filter.

中文：外量子效率（EQE）光谱使用 Enlitech QE-R 系统获得，并以经认证的硅参考电池进行校准。对于两端钙钛矿/硅叠层太阳能电池，硅底子电池的 EQE 使用 500 nm 短通滤光片测量，而钙钛矿顶子电池的 EQE 使用 850 nm 长通滤光片测量。

DoubleSAM-SAME2（PDF 第 5 页）

Original: We then operated solar cells as light-emitting diodes (Supplementary Fig. 22), and D-2P-treated PSC device showed enhanced electroluminescence (EL) intensity compared with S-2P-treated one. This directly demonstrates that non-radiative recombination at the interface between the perovskite and the transport layer is reduced in the D-2P-treated devices.

中文：随后我们将太阳能电池作为发光二极管运行（补充图 22），与 S-2P 处理的器件相比，D-2P 处理的 PSC 器件显示出增强的电致发光（EL）强度。这直接证明在 D-2P 处理器件中，钙钛矿与传输层之间界面处的非辐射复合被降低。

DoubleSAM-SAME2（PDF 第 6 页）

Original: To quantitatively evaluate and correlate the recombination rate with the Voc and device performance, we operated solar cells as light-emitting diodes (Fig. 4f), as follows: Voc = Voc,rad − kT/e lnEQEEL−1 (1) where Voc,rad, EQEEL, k, T and e are the radiative limit of Voc, electroluminescence external quantum efficiency, Boltzmann's constant, thermodynamic temperature and elementary charge.

中文：为了定量评估复合速率并将其与 Voc 及器件性能相关联，我们将太阳能电池作为发光二极管运行（图 4f），如下：Voc = Voc,rad − kT/e lnEQEEL−1（1），其中 Voc,rad、EQEEL、k、T 和 e 分别为 Voc 的辐射极限、电致发光外量子效率、玻尔兹曼常数、热力学温度和元电荷。

DoubleSAM-SAME2（PDF 第 7 页）

Original: The Voc loss was calculated by measuring the EQEEL of the device. D-2P-treated device obtained an improved EQEEL value (0.437%), which was an order of magnitude higher than S-2P-treated device (0.034%). This demonstrated the substantially reduced Voc loss of 0.15 V, agreeing well with the improved Voc of 1.32 V.

中文：Voc 损失通过测量器件的 EQEEL 来计算。D-2P 处理的器件获得了改进的 EQEEL 值（0.437%），比 S-2P 处理的器件（0.034%）高一个数量级。这表明 Voc 损失大幅降低了 0.15 V，与改善后的 1.32 V 的 Voc 吻合良好。

DoubleSAM-SAME2（PDF 第 7 页）

Original: The EL spectra of PSCs at various bias voltages are showed in the Fig. 5e, f. Distinguishable phase separation can be observed in S-2P-treated PSC when the bias voltage exceeds 3.0 V.

中文：PSC 在不同偏压下的 EL 光谱如图 5e、f 所示。当偏压超过 3.0 V 时，在 S-2P 处理的 PSC 中可以观察到明显的相分离。

DoubleSAM-SAME2（PDF 第 8 页）

Original: In contrast, D-2P-treated PSC exhibit continuously enhanced EL signals at constant wavelength with increasing bias voltage from 2.0 to 6.0 V. In addition to the improved electric field stability, the light stability of the D-2P-treated perovskite is also impressive.

中文：相比之下，随着偏压从 2.0 V 增加到 6.0 V，D-2P 处理的 PSC 在恒定波长处表现出持续增强的 EL 信号。除了改善的电场稳定性外，D-2P 处理钙钛矿的光稳定性也令人印象深刻。

DoubleSAM-SAME2（PDF 第 9 页）

Original: Electroluminescence efficiency (EQEEL) was performed via a system containing a Keithley 2400 digital source meter for current injection, a Keithley 6482 picometer, and the Si photodiode for quantifying the photons emitted from PSCs.

中文：电致发光效率（EQEEL）通过一个包含用于电流注入的 Keithley 2400 数字源表、Keithley 6482 皮安计以及用于量化 PSC 发射光子的硅光电二极管的系统进行测量。

5. 电化学阻抗谱、导纳与电容–电压特性（EIS / Admittance / C–V / Mott–Schottky）

DoubleSAM 2PACz Me-4PACz（PDF 第 7 页）

Original: We also conducted electron impedance spectroscopy (EIS) measurements to understand the transport mechanism of WBG devices, and the results are summarized in Table S3 (ESI†). The Nyquist plot (Fig. 4f) was obtained by measuring the control and target devices in dark with a bias voltage of 1.18 V and a sweep frequency range of 10 MHz to 10 Hz. The Me-4PACz interface molecular engineering led to a decrease in series resistance (RS) from 9.3 to 8.9 O and an increase in recombination resistance (Rrec) from 364.3 to 1253.4 O. Compared to the control ones, the target devices exhibit lower RS and higher Rrec in both low and high-frequency regions, indicating limited charge recombination and better carrier transport.

中文：我们还进行了电子阻抗谱（EIS）测量以理解 WBG 器件的传输机制，结果汇总于表 S3（ESI†）。Nyquist 图（图 4f）是在暗态下、偏压 1.18 V、扫描频率范围 10 MHz 至 10 Hz 的条件下测量对照组和目标器件得到的。Me-4PACz 界面分子工程使串联电阻（RS）从 9.3 降至 8.9 Ω，并使复合电阻（Rrec）从 364.3 增至 1253.4 Ω。与对照组相比，目标器件在低频和高频区域都表现出更低的 RS 和更高的 Rrec，表明电荷复合受到限制且载流子传输更好。

DoubleSAM 2PACz Me-4PACz（PDF 第 7 页）

Original: Capacitance–voltage (C–V) measurements were performed to estimate the built-in potential (Vbi) using Mott–Schottky analysis, as shown in Fig. 4g. The target devices exhibited a larger Vbi of 1.06 V compared to the control devices (0.95 V). The increase in Vbi is attributed to the suppression of non-radiative recombination through Me-4PACz interface molecular engineering.

中文：我们进行了电容–电压（C–V）测量，通过 Mott–Schottky 分析来估算内建电势（Vbi），如图 4g 所示。目标器件表现出更大的 Vbi，为 1.06 V，而对照组器件为 0.95 V。Vbi 的增加归因于 Me-4PACz 界面分子工程对非辐射复合的抑制。

DoubleSAM 2PACz Me-4PACz（PDF 第 7 页）

Original: The trap state density (Nt) was estimated using thermal admittance spectroscopy (TAS) measurements (Fig. 4h and Fig. S24, ESI†), revealing an NT of 2.19 1016 cm3 for the target perovskite film and 3.73 1016 cm3 for the control one.

中文：陷阱态密度（Nt）通过热导纳谱（TAS）测量进行估算（图 4h 和图 S24，ESI†），结果显示目标钙钛矿薄膜的 NT 为 2.19 × 10^16 cm−3，对照组为 3.73 × 10^16 cm−3。

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: From the electrochemical impedance spectroscopy (EIS) in Figure 3c, it is calculated that the device with BEpo-SAM has the higher recombination resistance (22 624 vs 36 472 Ω) and smaller series resistance (19.39 vs 11.25 Ω), which demonstrated less current leakage and efficient charge transport than the devices based on Me-4PACz.

中文：由图3c中的电化学阻抗谱（EIS）计算得到，采用BEpo-SAM的器件具有更高的复合电阻（22 624 对 36 472 Ω）和更小的串联电阻（19.39 对 11.25 Ω），这表明与基于Me-4PACz的器件相比，其电流泄漏更少、电荷传输更高效。

DoubleSAM3（PDF 第 5 页）

Original: To further probe the influence of different HTLs on interface charge dynamics, electrochemical impedance spectroscopy (EIS) was performed. Figure 3f shows the Nyquist plots of representative devices. The larger arc in the highfrequency region corresponds to the charge transfer process (charge transfer resistance, Rtr), while the smaller semicircle in the low-frequency region is associated with recombination behavior (recombination resistance, Rrec).37,38 Compared to the MeO-4PACz-based device, CbzBF-, CbzBT-, and CbzBF/CbzBT-based devices showed sequentially decreased Rtr and increased Rrec. The smallest Rtr and largest Rrec indicate that the CbzBF/CbzBT-based device effectively reduces nonradiative recombination and minimizes defect-assisted charge loss.

中文：为进一步探究不同 HTL 对界面电荷动力学的影响，我们进行了电化学阻抗谱（EIS）测试。图 3f 展示了代表性器件的 Nyquist 图。高频区较大的弧对应电荷转移过程（电荷转移电阻，Rtr），而低频区较小的半圆与复合行为相关（复合电阻，Rrec）。37,38 与基于 MeO-4PACz 的器件相比，基于 CbzBF、CbzBT 和 CbzBF/CbzBT 的器件表现出依次降低的 Rtr 和依次增大的 Rrec。最小的 Rtr 和最大的 Rrec 表明基于 CbzBF/CbzBT 的器件有效降低了非辐射复合并使缺陷辅助的电荷损失最小化。

DoubleSAM3（PDF 第 5 页）

Original: To elucidate the mechanism behind the enhanced Voc in devices with CbzBF/CbzBT bilayer, capacitance−voltage (C−V) analysis was carried out (Figure 3g). The built-in potential (Vbi) values for devices based on MeO-4PACz, CbzBF, CbzBT, and CbzBF/CbzBT were measured to be 1.05, 1.07, 1.08, and 1.12 V, respectively. A higher Vbi indicates a stronger built-in electric field, which facilitates the separation and extraction of photogenerated carriers.39

中文：为阐明 CbzBF/CbzBT 双层器件中 Voc 增强背后的机理，我们进行了电容–电压（C−V）分析（图 3g）。基于 MeO-4PACz、CbzBF、CbzBT 和 CbzBF/CbzBT 的器件的内建电势（Vbi）测得分别为 1.05、1.07、1.08 和 1.12 V。较高的 Vbi 表示更强的内建电场，有利于光生载流子的分离与提取。39

DoubleSAM3（PDF 第 7 页）

Original: Capacitance−voltage (C2−V) profiling was carried out to determine the net carrier concentration (NCV). The C2−V measurements were performed under dark conditions at room temperature using an AC frequency of 15 kHz and a modulation amplitude of 20 mV.

中文：进行了电容–电压（C2−V）剖面分析以确定净载流子浓度（NCV）。C2−V 测量在室温暗态条件下进行，使用 15 kHz 的交流频率和 20 mV 的调制幅度。

DoubleSAM-SAME2（PDF 第 5 页）

Original: We then measured the defect states of two perovskite films using thermal admittance spectroscopy (TAS). As shown, Band 1 ( < 0.4 eV) represents shallow level, Band 2 (0.4–0.5 eV) and Band 3 ( > 0.5 eV) represent deep level (Supplementary Fig. 21). Deep level defects are the main factors affecting device performance. The density of defect states (tDOS) was in the order of 1016 to 1019 m−3 eV−1 in the both devices. Meanwhile, the D-2P-treated perovskite device displayed the reduced tDOS over the entire trap depth compared with S-2P-treated film.

中文：随后我们使用热导纳谱（TAS）测量了两种钙钛矿薄膜的缺陷态。如图所示，带 1（< 0.4 eV）代表浅能级，带 2（0.4–0.5 eV）和带 3（> 0.5 eV）代表深能级（补充图 21）。深能级缺陷是影响器件性能的主要因素。两种器件的缺陷态密度（tDOS）均在 1016 至 1019 m−3 eV−1 数量级。同时，与 S-2P 处理薄膜相比，D-2P 处理的钙钛矿器件在整个陷阱深度范围内显示出降低的 tDOS。

DoubleSAM-SAME2（PDF 第 6 页）

Original: A similar conclusion could be also obtained from the capacitance-voltage (C-V) characteristics of PSCs (Fig. 4e). The D-2P-treated PSC displayed an increased built-in potential (Vbi) from 1.01 to 1.16 V, implying an enlarged driving force of carrier extraction and separation, which is contributing to the large Voc.

中文：从 PSC 的电容-电压（C-V）特性也可以得到类似的结论（图 4e）。D-2P 处理 PSC 显示出内建电势（Vbi）从 1.01 V 增加到 1.16 V，意味着载流子提取和分离的驱动力增大，这有助于实现大的 Voc。

6. 空间电荷限制电流与陷阱密度（SCLC / Trap density）

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: To probe the defect nature in the devices, the space charge limited current (SCLC) method that analyses the photovoltaic performance (I–V) of electron- or hole-only devices is a simple way, which can be usually divided into three regions: the Ohmic region with a linear increase in current and voltage in the low voltage range, a nonlinear polynomial increase within the range of the trap-filling limited (TFL) region at medium voltage and the trap position at the inflection point completely filled by charge carriers.

中文：为了探究器件中的缺陷性质，空间电荷限制电流（SCLC）方法——即分析电子单载流子或空穴单载流子器件的光伏性能（I–V）——是一种简便方法，通常可分为三个区域：低电压范围内电流随电压线性增加的欧姆区、中等电压下陷阱填充限制（TFL）区内的非线性多项式增加，以及在拐点处陷阱位置被电荷载流子完全填充。

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: The intermediate voltage range between the Ohmic region and the TFL region is called the trap-filling limited voltage (VTFL), and the trap density can be determined by the following equation:[46] VTFL = entL2 2𝜀r𝜀0 (1) where ɛr and ɛ0 are the relative dielectric constant of perovskite and vacuum permittivity, L is the thickness of perovskite film, and nt is the electron (hole) trap density of perovskite.

中文：欧姆区与TFL区之间的中间电压范围称为陷阱填充限制电压（VTFL），陷阱密度可由以下方程确定：[46] VTFL = entL2/2𝜀r𝜀0（1），其中ɛr和ɛ0分别为钙钛矿的相对介电常数和真空介电常数，L为钙钛矿薄膜的厚度，nt为钙钛矿的电子（空穴）陷阱密度。

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: In Figure 3a, the VTFL is deduced by the cross points of ohmic region and trap-filling region, which are 0.23 and 0.11 V for the devices based on Me-4PACz and BEpo-SAM, respectively. According to the equation, the calculated hole trap-state density is reduced from 1.13 × 1015 cm−3 (Me-4PACz) to 5.40 × 1014 cm−3 (BEpo-SAM).

中文：在图3a中，VTFL由欧姆区与陷阱填充区的交点推得，基于Me-4PACz和BEpo-SAM的器件分别为0.23 V和0.11 V。根据该方程，计算得到的空穴陷阱态密度从1.13 × 1015 cm−3（Me-4PACz）降低到5.40 × 1014 cm−3（BEpo-SAM）。

DoubleSAM2（PDF 第 7 页）

Original: Furthermore, we evaluated the influence of the BL-SAM strategy on the defect state density (Ntrap) through space-charge-limited current (SCLC) measurements. As shown in Figure 5b, the trap-filled limit voltage (VTFL) is defined as the voltage at the transition point between the ohmic and trap-filled regions. The Ntrap is obtained via the following formula [41, 53]: Ntrap = 2𝜀r𝜀0VTFL qL2 (4) where εr represents the relative dielectric constant, ε0 denotes the vacuum dielectric constant, q stands for the elementary charge, and L corresponds to the thickness of the perovskite film.

中文：此外，我们通过空间电荷限制电流（SCLC）测量评估了BL-SAM策略对缺陷态密度（Ntrap）的影响。如图5b所示，陷阱填充极限电压（VTFL）定义为欧姆区与陷阱填充区之间转变点处的电压。Ntrap由以下公式获得 [41, 53]：Ntrap = 2𝜀r𝜀0VTFL/qL2 (4)，其中εr代表相对介电常数，ε0表示真空介电常数，q代表元电荷，L对应钙钛矿薄膜的厚度。

DoubleSAM2（PDF 第 7 页）

Original: The BL-SAM device achieved the lowest VTFL, at only 0.17 V, which also signifies that it has the lowest Ntrap [52, 54], indicating that the defect density is distinctly reduced within the PSCs [55, 56].

中文：BL-SAM器件实现了最低的VTFL，仅为0.17 V，这也意味着它具有最低的Ntrap [52, 54]，表明PSC中的缺陷密度明显降低 [55, 56]。

DoubleSAM3（PDF 第 5 页）

Original: To evaluate the defect state density and charge carrier recombination behavior at the perovskite/HTL interface, we conducted space charge limited current (SCLC) measurements on hole-only devices (ITO/HTLs/perovskite/PTAA/Ag) (Figure 3e). The transition point between the ohmic region and the trap-filling region in the current−voltage curve corresponds to the trap-filling limit voltage (VTFL).25 The VTFL values for devices based on MeO-4PACz, CbzBF, CbzBT, and CbzBF/CbzBT were 1.04, 0.99, 0.89, and 0.64 V, respectively.

中文：为评估钙钛矿/HTL 界面的缺陷态密度和电荷载流子复合行为，我们对单空穴器件（ITO/HTLs/perovskite/PTAA/Ag）进行了空间电荷限制电流（SCLC）测量（图 3e）。电流–电压曲线中欧姆区与陷阱填充区之间的转变点对应陷阱填充极限电压（VTFL）。基于 MeO-4PACz、CbzBF、CbzBT 和 CbzBF/CbzBT 的器件的 VTFL 值分别为 1.04、0.99、0.89 和 0.64 V。

DoubleSAM3（PDF 第 5 页）

Original: The defect state density (Nt) can be calculated using the following equation: = N V ed 2 t 0 TFL 2 (3) where ε is the relative permittivity of the perovskite, ε0 is the vacuum permittivity, e is the elementary charge, and d is the thickness of the perovskite layer. A lower VTFL indicates a reduced trap state density, as Nt is positively correlated with VTFL. The device with CbzBF/CbzBT exhibited the lowest VTFL, confirming the lowest defect density in devices.

中文：缺陷态密度（Nt）可用以下公式计算：= N V ed 2 t 0 TFL 2 (3)，其中 ε 是钙钛矿的相对介电常数，ε0 是真空介电常数，e 是元电荷，d 是钙钛矿层的厚度。较低的 VTFL 表示陷阱态密度降低，因为 Nt 与 VTFL 正相关。采用 CbzBF/CbzBT 的器件表现出最低的 VTFL，证实了器件中最低的缺陷密度。

DoubleSAM3（PDF 第 7 页）

Original: The space-charge-limited current (SCLC) characteristics of the perovskite devices were evaluated using a commercial measurement system (XPQY-eq E- 350-1100, Guangzhou Xipu Optoelectronics Technology) equipped with an integrating sphere (Labsphere GPS-4P-SL) and a photodetector array (Hamamatsu S7031−1006).

中文：钙钛矿器件的空间电荷限制电流（SCLC）特性使用商用测量系统（XPQY-eq E-350-1100，广州溪普光电技术）进行评估，该系统配备积分球（Labsphere GPS-4P-SL）和光电探测器阵列（Hamamatsu S7031−1006）。

7. 瞬态光电流与瞬态光电压（TPC / TPV）

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: The charge extraction was characterized by transient photocurrent decay (Figure 3d) and the photocurrent decay decreased from 5.28 μs (Me-4PACz) to 3.10 μs (BEpo-SAM). The above results demonstrated the reduced nonradiative charge recombination and more efficient charge extraction and transport in the devices based on BEpo-SAM.

中文：电荷提取通过瞬态光电流衰减进行表征（图3d），光电流衰减时间从5.28 μs（Me-4PACz）缩短到3.10 μs（BEpo-SAM）。上述结果表明，基于BEpo-SAM的器件中非辐射电荷复合减少，电荷提取与传输更为高效。

DoubleSAM2（PDF 第 7 页）

Original: To further analyze the charge recombination behavior within the devices, we performed transient photovoltage (TPV) (Figure 5c) and transient photocurrent (TPC) (Figure S25) measurements. A longer carrier lifetime indicates lower recombination losses, while a shorter charge extraction time suggests higher charge collection efficiency at the electrodes [57–60]. Notably, the prolonged carrier lifetime (4.72 µs) and shortened extraction time (1.79 µs) observed in the BL-SAM device confirm suppressed internal recombination and enhanced charge transport efficiency [59–61]. Thus, these favorable kinetic parameters constitute the mechanistic basis for the superior FF value [42].

中文：为进一步分析器件内的电荷复合行为，我们进行了瞬态光电压（TPV）（图5c）和瞬态光电流（TPC）（图S25）测量。更长的载流子寿命表明更低的复合损失，而更短的电荷提取时间表明电极处具有更高的电荷收集效率 [57–60]。值得注意的是，BL-SAM器件中观察到的延长载流子寿命（4.72 µs）和缩短提取时间（1.79 µs）证实了内部复合被抑制、电荷输运效率提高 [59–61]。因此，这些有利的动力学参数构成了优异FF值的机理基础 [42]。

DoubleSAM-SAME2（PDF 第 6 页）

Original: Therefore, a longer charge-recombination lifetime (τrec = 53.33 μs) and a shorter charge-extraction time (τtra = 0.38 μs) were obtained according to the transient photovoltage (TPV) and transient photocurrent (TPC) measurements (Supplementary Fig. 39).

中文：因此，根据瞬态光电压（TPV）和瞬态光电流（TPC）测量（补充图 39），获得了更长的电荷复合寿命（τrec = 53.33 μs）和更短的电荷提取时间（τtra = 0.38 μs）。

8. 循环伏安与分子覆盖密度（CV / Molecular density）

DoubleSAM-SAME（PDF 第 5 页）

Original: To overcome these limitations and selectively probe the removal of first-layer SAMs, we turned to CV, an electrochemical technique that is inherently first-layer sensitive; that is, it quantifies the areal density of electrochemically active molecules, such as carbazole-based SAMs, that are directly coupled to the electrode surface (Figures S23−S31).

中文：为克服这些局限并选择性地探测第一层SAM的去除，我们转向CV——一种本质上对第一层敏感的电化学技术；也就是说，它定量的是直接与电极表面耦合的电化学活性分子（如咔唑基SAM）的面密度（图S23−S31）。

DoubleSAM-SAME（PDF 第 5 页）

Original: Unlike XPS, CV selectively probes molecules that are either (i) directly adsorbed onto the ITO surface38 or (ii) positioned close enough to ITO to allow efficient electron tunneling, typically within 1.5 nm of the surface.39

中文：与XPS不同，CV选择性地探测那些（i）直接吸附在ITO表面上的分子，或（ii）位置足够靠近ITO以实现高效电子隧穿的分子，通常位于距表面1.5 nm以内。

DoubleSAM-SAME（PDF 第 6 页）

Original: CV results shown in Figure 3c demonstrate that ethanol washing reduces MeO-2PACz areal density from 0.307 to 0.262 molecules nm−2 (a 15% reduction), while DMF washing leads to a more pronounced decrease to 0.206 molecules nm−2 (a 33% reduction).

中文：图3c所示的CV结果表明，乙醇清洗将MeO-2PACz面密度从0.307降低到0.262分子 nm−2（降低15%），而DMF清洗导致更明显的下降，降至0.206分子 nm−2（降低33%）。

DoubleSAM-SAME（PDF 第 6 页）

Original: We first note that while XPS shows nearly identical overall decreases in SAM abundance for ethanol and DMF treatments (a 3% difference in the N/In ratio), CV reveals a much larger difference between the two (a 10% difference in areal density). Given that both solvents are able to remove loosely bound molecules in secondary layers, this difference suggests the presence of a multilayered SAM structure, with a substantial fraction of molecules extending beyond the first monolayer.

中文：我们首先注意到，虽然XPS显示乙醇和DMF处理对SAM总量的整体降幅几乎相同（N/In比值相差3%），但CV显示二者之间存在大得多的差异（面密度相差10%）。鉴于两种溶剂都能去除二次层中松散结合的分子，这一差异表明SAM呈现多层结构，其中相当一部分分子延伸到第一单层之外。

DoubleSAM-SAME（PDF 第 6 页）

Original: Additionally, the stronger reduction in CV-derived areal density after DMF washing (33%) indicates that DMF is far more effective than ethanol (15%) at removing weakly bound molecules directly adsorbed to the ITO surface. For 2PACz and 4PADCB (Figure S35), the overall trends mirror those observed for MeO-2PACz.

中文：此外，DMF清洗后CV测得的面密度降低幅度更大（33%），表明DMF在去除直接吸附在ITO表面的弱结合分子方面远比乙醇（15%）有效。对于2PACz和4PADCB（图S35），总体趋势与MeO-2PACz一致。

DoubleSAM-SAME（PDF 第 6 页）

Original: These combined XPS and CV results suggest that ethanol removes a relatively small fraction of SAM molecules (15−37%), corresponding to the very weakly bound molecules such as carbazole-bound species. In contrast, DMF removes 31−47% of the SAM molecules by stripping away not only these very weakly bound molecules but also moderately bound ones such as those stabilized by hydrogen bonding. We further conclude that the first-layer SAM molecules that remain intact after DMF washing (53−69%) correspond to those that are covalently bound to the ITO surface.

中文：这些XPS与CV的综合结果表明，乙醇去除了相对较小比例的SAM分子（15−37%），对应于极弱结合的分子，如通过咔唑基团结合的物种。相比之下，DMF去除了31−47%的SAM分子，不仅剥离了这些极弱结合的分子，还去除了中等结合的分子，例如通过氢键稳定的分子。我们进一步得出结论：DMF清洗后仍完好保留的第一层SAM分子（53−69%）对应于共价结合在ITO表面上的那些分子。

DoubleSAM-SAME（PDF 第 8 页）

Original: XPS was then employed to measure the total molecular abundance across multilayered SAMs, while CV was used to selectively measure the density of molecules in the first monolayer. This dual characterization revealed that DMF washing removes over 50% of SAMs, including a substantial reduction in the first layer, through displacement of weakly bound species.

中文：随后使用XPS测量多层SAM的总分子丰度，而使用CV选择性地测量第一单层中的分子密度。这种双表征揭示，DMF清洗通过置换弱结合物种去除了超过50%的SAM，包括第一层中的显著减少。

9. 电导率与电荷迁移率（Conductivity / Mobility）

DoubleSAM2（PDF 第 5 页）

Original: To further characterize the charge transport properties, the conductivity (σ) was calculated using the following formula [20, 27]: 𝜎= 𝑑 𝐴𝑅 (1) where d is the SAM layer thickness, A is the active device area, and R is the resistance derived from J–V curves.

中文：为进一步表征电荷输运性质，电导率（σ）由以下公式计算 [20, 27]：𝜎= 𝑑/𝐴𝑅 (1)，其中d为SAM层厚度，A为器件有效面积，R为由J–V曲线得到的电阻。

DoubleSAM2（PDF 第 5 页）

Original: As shown in Figure S15, the BL-SAM delivered significantly higher in-plane conductivity with 1.4 × 10−6 S/cm relative to both Me-4PACz (6.0 × 10−7 S/cm) and MeO-4PADCB (5.8 × 10−7 S/cm). This improved conductivity is attributed to the formation of a denser and more uniform molecular, which contributes to enhanced charge carrier mobility [28].

中文：如图S15所示，BL-SAM表现出显著更高的面内电导率，为1.4 × 10−6 S/cm，而Me-4PACz（6.0 × 10−7 S/cm）和MeO-4PADCB（5.8 × 10−7 S/cm）均较低。这种电导率的改善归因于形成了更致密、更均匀的分子层，有助于提高电荷载流子迁移率 [28]。

DoubleSAM-SAME2（PDF 第 7 页）

Original: We evaluated the migration ability of halide ions by temperature-dependent conductivity measurements. The ion migration activation energy (Ea) is obtained by fitting the corresponding plots with the Nernst-Einstein equation (Fig. 5d). A larger Ea (0.58 eV) is observed in the D-2P-treated perovskite film than that in the S-2P-treated one (0.17 eV). The relieved lattice strain and increased halogen ion migration barrier facilitate the realization of robust stability of mixed-halide perovskite films.

中文：我们通过温度依赖的电导率测量评估了卤化物离子的迁移能力。离子迁移活化能（Ea）通过用 Nernst-Einstein 方程拟合相应曲线获得（图 5d）。在 D-2P 处理的钙钛矿薄膜中观察到比 S-2P 处理薄膜（0.17 eV）更大的 Ea（0.58 eV）。缓解的晶格应变和增大的卤素离子迁移势垒有助于实现混合卤化物钙钛矿薄膜的稳健稳定性。

10. 开路电压衰减与光强依赖电学分析（OCVD / Light-intensity dependence）

DoubleSAM 2PACz Me-4PACz（PDF 第 7 页）

Original: To investigate the impact of Me-4PACz interface engineering on charge recombination, we conducted light intensitydependent J–V measurements. As shown in Fig. 4e, VOC exhibits a logarithmic increase with increasing light intensity. The relationship was fitted using eqn (1): VOC = nkT ln(L)/q (1) where n, k, T, L, and q represent the ideality factor, Boltzmann’s constant, absolute temperature, light intensity, and elementary charge, respectively.

中文：为研究 Me-4PACz 界面工程对电荷复合的影响，我们进行了光强依赖的 J–V 测量。如图 4e 所示，VOC 随光强增加呈对数增长。该关系用式 (1) 拟合：VOC = nkT ln(L)/q (1)，其中 n、k、T、L 和 q 分别代表理想因子、玻尔兹曼常数、绝对温度、光强和元电荷。

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: Additionally, the light intensity-dependent Voc is plotted (Figure 3b) and the fitting relationship is:[47,48] VOC = nkT ln L∕q (2) where n, k, T, L, and q represent the ideality factor, Boltzmann constant, absolute temperature, light intensity, and elementary charge, respectively.

中文：此外，绘制了依赖于光强的Voc（图3b），其拟合关系为：[47,48] VOC = nkT ln L∕q（2），其中n、k、T、L和q分别代表理想因子、玻尔兹曼常数、绝对温度、光强和元电荷。

DoubleSAM Me-4PACz Br-EPA（PDF 第 4 页）

Original: The device with BEpo-SAM shows the smaller ideality factor of 1.38 than that of the device with Me-4PACz (1.52), indicating suppressed Shockley–Read–Hall recombination at the interface because of the voids filling and defects passivation.

中文：采用BEpo-SAM的器件表现出更小的理想因子1.38，小于采用Me-4PACz的器件（1.52），这表明由于空洞填充和缺陷钝化，界面处的Shockley–Read–Hall复合被抑制。

DoubleSAM2（PDF 第 7 页）

Original: To assess comprehensive assessment of the carrier dynamics and defect passivation, the dependence of VOC on light intensity was investigated, as depicted in Figure 5a. The relationship between VOC and light intensity can be described by the formula [39, 40, 50]: Voc = nKBT q ln (I) + A (3) where n, KB, T, q, I and A represent the diode ideality factor, Boltzmann constant, temperature in Kelvin, elementary charge, light intensity and a constant, respectively. The BL-SAM device exhibited an n of 1.60, which is lower than the values of 1.95 and 1.74 measured for Me-4PACz and MeO-4PADCB devices, respectively. The lower n value indicates diminished trap-assisted recombination, indicating effective suppression of Shockley-Read-Hall recombination pathways [51, 52].

中文：为全面评估载流子动力学和缺陷钝化，我们研究了VOC对光强的依赖性，如图5a所示。VOC与光强之间的关系可用以下公式描述 [39, 40, 50]：Voc = nKBT/q ln(I) + A (3)，其中n、KB、T、q、I和A分别代表二极管理想因子、玻尔兹曼常数、开尔文温度、元电荷、光强和常数。BL-SAM器件的n为1.60，低于Me-4PACz和MeO-4PADCB器件测得的1.95和1.74。较低的n值表明陷阱辅助复合减少，说明Shockley-Read-Hall复合路径被有效抑制 [51, 52]。

DoubleSAM-SAME2（PDF 第 6 页）

Original: The dependence of Voc on illumination intensity is an effective strategy to evaluate the internal recombination mechanism in PSCs. The ideality factor n can be obtained by calculating the slope of the fitted straight line. As shown in Fig. 4d, D-2P-treated PSC displayed a smaller n value (1.21) than S-2P-treated PSC (1.88), and n value close to 1 indicates that Shockley-Read-Hall recombination is substantially suppressed.

中文：Voc 对光照强度的依赖性是评估 PSC 内部复合机制的有效策略。理想因子 n 可通过计算拟合直线的斜率获得。如图 4d 所示，D-2P 处理 PSC 显示出比 S-2P 处理 PSC（1.88）更小的 n 值（1.21），而接近 1 的 n 值表明 Shockley-Read-Hall 复合被大幅抑制。

11. 最大功率点跟踪与器件电学稳定性（MPPT / Operational & reverse-bias stability）

Poly-SAM（PDF 第 6 页）

Original: Both the control and target devices exhibited excellent operational stability, retaining over 90% of their initial PCE after 1,000 h 1-sun MPPT (following the International Summit on Organic Solar Cell Stability protocol for light-soaking stability testing under continuous 1-sun illumination at ambient temperature and ambient atmosphere (ISOS-L-1), Fig. 3d). The slightly enhanced operational stability of the target device is attributed to the improved robustness at the buried interface that minimizes ion migration.

中文：对照和目标器件都表现出优异的运行稳定性，在 1,000 h 的 1 个太阳 MPPT 后仍保持其初始 PCE 的 90% 以上（遵循国际有机太阳能电池稳定性峰会关于在环境温度和环境气氛下连续 1 个太阳光照的光浸泡稳定性测试协议（ISOS-L-1），图 3d）。目标器件运行稳定性略有提升，归因于埋底界面稳健性的改善，从而最小化离子迁移。

Poly-SAM（PDF 第 6 页）

Original: Regarding damp–heat stability (International Summit on Organic Solar Cell Stability protocol for dark-storage stability testing under 85 oC and 85% RH (ISOS-D-3), Fig. 3e), the target device retained 91% of its initial PCE, while the control device kept only 80% after ageing for 1,100 h, indicating that the PTP-SAM exhibits better thermal stability through a stronger interaction with the ITO substrate.

中文：关于湿热稳定性（国际有机太阳能电池稳定性峰会关于在 85 oC 和 85% RH 下暗态储存稳定性测试协议（ISOS-D-3），图 3e），目标器件在老化 1,100 h 后保持其初始 PCE 的 91%，而对照器件仅保持 80%，表明 PTP-SAM 通过与 ITO 基底更强的相互作用表现出更好的热稳定性。

Poly-SAM（PDF 第 7 页）

Original: We evaluated the long-term stability of devices under a continuous reverse bias of −4.8 V (see Methods for details), approximately four times the ISOS-V-1 specification33, enabling accelerated testing. The control devices retained only 66% of their initial PCE after 12 h, while the target devices maintained 95% of their initial PCE after ageing for 300 h (Fig. 3h).

中文：我们评估了器件在 −4.8 V 连续反向偏压下的长期稳定性（详见方法部分），该电压约为 ISOS-V-1 规范的四倍，从而实现加速测试。对照器件在 12 h 后仅保持其初始 PCE 的 66%，而目标器件在老化 300 h 后仍保持其初始 PCE 的 95%（图 3h）。

Poly-SAM（PDF 第 7 页）

Original: Considering multifactorial stress in real-world operation, we initiated combined stressor tests (−VOC reverse bias plus 85 °C with an environmental relative humidity (RH) of 88%) to evaluate the stability under more practical conditions (Supplementary Fig. 49). The PTP-SAM device showed a T80 (T80 is defined as the time required for the device performance to decay to 80% of its initial value) lifetime of 9 h, whereas the SAM device degraded more rapidly, dropping to 65% of its original performance after only 1 h and breaking down completely after 2 h. These results, consistent with our single stressor tests, further demonstrate the robustness of the PTP-SAM strategy.

中文：考虑到实际运行中的多因素应力，我们启动了组合应力测试（−VOC 反向偏压加 85 °C、环境相对湿度（RH）88%），以评估更实际条件下的稳定性（补充图 49）。PTP-SAM 器件表现出 9 h 的 T80（T80 定义为器件性能衰减至其初始值 80% 所需的时间）寿命，而 SAM 器件退化更快，仅在 1 h 后就降至其原始性能的 65%，并在 2 h 后完全击穿。这些结果与我们单一应力测试一致，进一步证明了 PTP-SAM 策略的稳健性。

Poly-SAM（PDF 第 7 页）

Original: As PSCs are scaled up, increased current leakage at the buried interface due to direct perovskite–electrode contact amplifies performance loss and reverse-bias degradation. Therefore, perovskite solar modules (PSMs) with an aperture area of 20.25 cm2 were fabricated to demonstrate the effect of PTP-SAM over a larger area.

中文：随着 PSC 的放大，由于钙钛矿与电极直接接触导致的埋底界面漏电流增加，会放大性能损失和反向偏压降解。因此，制备了孔径面积为 20.25 cm2 的钙钛矿太阳能组件（PSM），以在更大面积上展示 PTP-SAM 的效果。

Poly-SAM（PDF 第 8 页）

Original: To evaluate the reverse-bias stability at the minimodule scale, we applied a constant reverse voltage of −VOC (−9.5 V) to both control and target PSMs and monitored the evolution of PCE over time following the ISOS-V-1 protocol (see Supplementary Fig. 54 for a photograph of the set-up). The control PSMs exhibited rapid degradation, retaining only 78% of their initial PCE after ageing for 12 h, whereas the target PSMs maintained 98% of their original performance after 312 h, demonstrating excellent robustness under reverse-bias stress (Fig. 4g, Supplementary Fig. 55 and Supplementary Note 8). For comparison, previously reported PSMs retained only 84% of their initial performance after just 1 h under −VMPP bias35.

中文：为评估微型组件尺度的反向偏压稳定性，我们对对照和目标 PSM 施加了恒定的反向电压 −VOC（−9.5 V），并按照 ISOS-V-1 协议监测 PCE 随时间的变化（装置照片见补充图 54）。对照 PSM 迅速退化，老化 12 h 后仅保持其初始 PCE 的 78%，而目标 PSM 在 312 h 后仍保持其原始性能的 98%，显示出在反向偏压应力下优异的稳健性（图 4g、补充图 55 和补充说明 8）。作为比较，此前报道的 PSM 在 −VMPP 偏压下仅 1 h 后就仅保持其初始性能的 84%。

Poly-SAM（PDF 第 8 页）

Original: To further validate the effectiveness of our strategy, we subjected a single subcell (out of eight) to partial shading and aged the minimodules under 1-sun illumination at 55 ± 5 °C in a short-circuit state (see Supplementary Figs. 56 and 57 for photographs of the set-up and equivalent circuit diagram). Under these conditions, the shaded subcell experienced the highest reverse stress with a reverse voltage of −7 × VCell,SC (the voltage of each subcell at short-circuit condition) to accelerate ageing (Supplementary Fig. 57). The control device degraded to below 80% of its initial PCE within just 1 h, whereas the target PSM retained 90% of its original PCE after ageing for 8 h (Supplementary Fig. 58).

中文：为进一步验证我们策略的有效性，我们对八个子电池中的一个进行部分遮挡，并在 1 个太阳光照、55 ± 5 °C 下以短路状态对微型组件进行老化（装置照片和等效电路图见补充图 56 和 57）。在这些条件下，被遮挡的子电池承受最高的反向应力，反向电压为 −7 × VCell,SC（每个子电池在短路条件下的电压），以加速老化（补充图 57）。对照器件在仅 1 h 内就退化到低于其初始 PCE 的 80%，而目标 PSM 在老化 8 h 后仍保持其原始 PCE 的 90%（补充图 58）。

Poly-SAM（PDF 第 8 页）

Original: We simulated a more realistic scenario in which a subcell was shaded while the module operated at its maximum power point. If the subcell underwent breakdown, the output current of the entire module would rapidly rise to the module current at maximum power point (IMPP) (refs. 15,36). We monitored the current of a 16-subcell PTP-SAM module with one subcell shaded under 1-sun illumination at VMPP (Supplementary Fig. 59). The current output remained at a low level (average current Iavg = −456.1 μA) for 14 h, without current leakage to the milliampere level or sudden breakdown to IMPP. Meanwhile, the module retained 97% of its initial performance (Supplementary Fig. 60). This indicates that only one single bypass diode can effectively protect a perovskite module with at least 16 subcells under real operating conditions (Fig. 4h).

中文：我们模拟了一个更真实的场景：模块在其最大功率点运行时一个子电池被遮挡。如果该子电池发生击穿，整个模块的输出电流将迅速上升到最大功率点处的模块电流（IMPP）。我们监测了一个 16 子电池 PTP-SAM 模块在 1 个太阳光照下 VMPP 运行、其中一个子电池被遮挡时的电流（补充图 59）。电流输出在 14 h 内保持低水平（平均电流 Iavg = −456.1 μA），没有漏电流升至毫安级，也没有突然击穿至 IMPP。同时，该模块保持其初始性能的 97%（补充图 60）。这表明仅一个单个旁路二极管就能在实际运行条件下有效保护具有至少 16 个子电池的钙钛矿模块（图 4h）。

Poly-SAM（PDF 第 9 页）

Original: MPPT measurements of the encapsulated devices were recorded using an MPP Tracking-4B system (Shenzhen Lancheng Technology) and an AM1.5G spectrum simulated with a light-emitting diode (LED). Measurements were carried out under ambient conditions at ~45 °C with an RH of 85% (ISOS-L-1).

中文：封装器件的 MPPT 测量使用 MPP Tracking-4B 系统（深圳蓝城科技）和由发光二极管（LED）模拟的 AM1.5G 光谱记录。测量在约 45 °C、RH 85% 的环境条件下进行（ISOS-L-1）。

Poly-SAM（PDF 第 9 页）

Original: As shown in Fig. 3h, each data point was collected by I–V scanning after the following treatment: (1) biasing the small-area solar cell at −4.8 V in a dark, nitrogen-filled glove box for 12 h (ISOS-V-1), (2) recovery in the dark for 10 h and (3) light soaking under 1-sun illumination for 30 min before measurement. The pre- and post-recovery data, as well as the evolution of the reverse current for 12 h in one cycle, are presented in Supplementary Figs. 61 and 62.

中文：如图 3h 所示，每个数据点均通过以下处理后的 I–V 扫描收集：（1）在暗态充氮手套箱中将小面积太阳能电池偏置在 −4.8 V 下 12 h（ISOS-V-1），（2）在暗态中恢复 10 h，（3）测量前在 1 个太阳光照下光浸泡 30 min。恢复前后的数据以及一个循环中 12 h 的反向电流演化见补充图 61 和 62。

Poly-SAM（PDF 第 9 页）

Original: As shown in Fig. 4g, each data point was collected by I–V scanning after the following treatment: (1) biasing the PSM at −9.5 V in a dark, nitrogen-filled glove box for 12 or 24 h for (ISOS-V-1), (2) recovery in the dark for 12 h and (3) light soaking under 1-sun illumination for 30 min before measurement.

中文：如图 4g 所示，每个数据点均通过以下处理后的 I–V 扫描收集：（1）在暗态充氮手套箱中将 PSM 偏置在 −9.5 V 下 12 或 24 h（ISOS-V-1），（2）在暗态中恢复 12 h，（3）测量前在 1 个太阳光照下光浸泡 30 min。

Poly-SAM（PDF 第 9 页）

Original: As shown in Supplementary Fig. 58, each data point was collected by I–V scanning after the following treatment: (1) the shaded PSM was placed in short-circuit conditions under 1-sun illumination at 55 ± 5 °C inside a nitrogen-filled glove box for 1 h (ISOS-V-2) and (2) the shaded mask was removed and recovered in the dark for 1 h before measurement.

中文：如补充图 58 所示，每个数据点均通过以下处理后的 I–V 扫描收集：（1）将被遮挡的 PSM 置于充氮手套箱中，在 1 个太阳光照、55 ± 5 °C 下保持短路条件 1 h（ISOS-V-2），（2）移除遮挡掩模并在暗态中恢复 1 h 后进行测量。

DoubleSAM 2PACz Me-4PACz（PDF 第 6 页）

Original: We performed maximum power point tracking (MPPT) measurements for both the control and target devices, as recorded in Fig. S22 (ESI†). It shows that the efficiency of the target device remains at 80% of the initial PCE after 400 h, while the efficiency of the control device drops to 80% of the initial PCE after 200 h.

中文：我们对对照组和目标器件都进行了最大功率点跟踪（MPPT）测量，结果记录于图 S22（ESI†）。结果表明，目标器件的效率在 400 h 后仍保持在初始 PCE 的 80%，而对照器件的效率在 200 h 后就下降到初始 PCE 的 80%。

DoubleSAM 2PACz Me-4PACz（PDF 第 7 页）

Original: This enhancement in stability can be primarily attributed to several factors. First, compared to the unevenly distributed and porous perovskite layer formed by 2PACz, the interaction of the phosphate functional group of Me-4PACz with PbI2/PbBr2 leads to the formation of a dense buried interface. This interface improves the structural stability of the perovskite film by releasing stress and promoting a higher degree of crystallinity. A more crystalline and stable perovskite film is less prone to degradation, leading to improved long-term stability of the device. Furthermore, the reduction of non-radiative recombination centers plays a crucial role in stabilizing the device performance. The Me-4PACz interface engineering effectively suppresses non-radiative recombination processes by reducing trap densities and improving charge carrier dynamics. This improvement allows for more efficient extraction and transport of charge carriers, minimizing energy losses and enhancing the stability of the device during prolonged operation. Overall, the combination of improved structural stability and reduced non-radiative recombination centers provided by the Me-4PACz interface engineering contributes to the enhanced stability observed in the target cells.

中文：这种稳定性提升主要可归因于几个因素。第一，与由 2PACz 形成的分布不均且多孔的钙钛矿层相比，Me-4PACz 的磷酸官能团与 PbI2/PbBr2 的相互作用形成了致密的埋底界面。该界面通过释放应力并促进更高的结晶度改善了钙钛矿薄膜的结构稳定性。结晶度更高、更稳定的钙钛矿薄膜更不易降解，从而提升了器件的长期稳定性。此外，非辐射复合中心的减少对稳定器件性能起着关键作用。Me-4PACz 界面工程通过降低陷阱密度和改善载流子动力学，有效抑制了非辐射复合过程。这一改善使载流子能够更高效地提取与传输，从而将能量损失降至最低，并增强器件在长时间运行中的稳定性。总体而言，Me-4PACz 界面工程所带来的结构稳定性提升与非辐射复合中心减少共同促成了目标电池中观察到的稳定性增强。

DoubleSAM 2PACz Me-4PACz（PDF 第 8 页）

Original: To achieve more reliable device performance, the steady-state power output of the device was measured at the maximum power point (1.14 V for the semi-transparent WBG device and 0.74 V for the filtered NBG device) over 250 s (Fig. 5h). The stable output of the semi-transparent WBG device and the filtered NBG bottom cell reached stabilized PCE values of 17.99% and 9.71%, respectively, closely matching the values obtained from the J–V curve.

中文：为获得更可靠的器件性能，我们在最大功率点处（半透明 WBG 器件为 1.14 V，滤光后的 NBG 器件为 0.74 V）对器件的稳态功率输出进行了 250 s 的测量（图 5h）。半透明 WBG 器件和滤光后的 NBG 底电池的稳定输出分别达到 17.99% 和 9.71% 的稳定 PCE 值，与由 J–V 曲线得到的值非常接近。

DoubleSAM Me-4PACz Br-EPA（PDF 第 5 页）

Original: The dense SAM, the defects passivation, and the improved crystallinity of perovskite have been reported to enhance the operation stability of PSCs. Here, we verified the operation stability of our devices in Figure 4d. The encapsulated device based on BEpo-SAM maintained ca. 90% of the initial PCE (24.92%) after 1000 h of operation at the maximum power point (MPP), under 1sun illumination and 40 °C, whereas the PCE of the device based on Me-4PACz dropped by 51% after 600 h of operation under the same conditions.

中文：据报道，致密的SAM、缺陷钝化以及钙钛矿结晶度的改善可增强PSC的运行稳定性。在此，我们在图4d中验证了器件的运行稳定性。基于BEpo-SAM的封装器件在1个太阳光照和40 °C下于最大功率点（MPP）运行1000 h后，仍保持初始PCE（24.92%）的约90%，而基于Me-4PACz的器件在相同条件下运行600 h后PCE下降了51%。

DoubleSAM Me-4PACz Br-EPA（PDF 第 5 页）

Original: To examine the storage stability of the devices, the devices were kept in a dark dry box with relative humidity of <5% and room temperature for 8 weeks (Figure 4e). For the device based on BEpo-SAM, the efficiency increased from 24.50% to 25.05%. As for the device based on Me-4PACz, an increase in the efficiency can also be found in the first 2 weeks, whereas it went through a gradual drop and maintained 81% of the initial PCEs after 8 weeks.

中文：为考察器件的储存稳定性，将器件置于相对湿度<5%、室温的黑暗干燥箱中8周（图4e）。对于基于BEpo-SAM的器件，效率从24.50%提高到25.05%。而对于基于Me-4PACz的器件，前2周效率也有所提高，但随后逐渐下降，8周后保持初始PCE的81%。

DoubleSAM2（PDF 第 8 页）

Original: As illustrated in Figure 5d, humidity stability was evaluated by exposing unencapsulated devices under ambient environmental conditions (25◦C and RH of 40%). After 960 h of exposure, the BL-SAM modified device maintained 81% of its initial PCE, in contrast to the control devices, which degraded to 48% and 36%, respectively.

中文：如图5d所示，湿度稳定性通过将未封装器件暴露于环境条件（25◦C、相对湿度40%）下进行评估。暴露960 h后，BL-SAM修饰器件保持其初始PCE的81%，而对照器件分别衰减到48%和36%。

DoubleSAM2（PDF 第 8 页）

Original: As shown in Figure 5e, thermal stability was examined under an inert nitrogen atmosphere at an elevated temperature of 85◦C. After 864 h of thermal aging, the BL-SAM devices retained approximately 80% of their initial PCE, while the control counterparts exhibited substantial degradation, maintaining only 49% and 43% of their original efficiencies, respectively.

中文：如图5e所示，热稳定性在85◦C的惰性氮气气氛下进行考察。经过864 h热老化后，BL-SAM器件保持其初始PCE的约80%，而对照器件表现出显著衰减，分别仅保持其原始效率的49%和43%。

DoubleSAM2（PDF 第 8 页）

Original: Additionally, according to the ISOS-L-1 protocol, MPP tracking stability measurements were carried out under continuous one-sun illumination at 30 ± 5◦C, as presented in Figure 5f. After 400 h of continuous light exposure, the BL-SAM device retained 87% of its initial performance, whereas the efficiencies of the reference devices decreased to 63% and 59%.

中文：此外，根据ISOS-L-1协议，在30 ± 5◦C下连续单太阳光照下进行了MPP跟踪稳定性测量，如图5f所示。经过400 h连续光照后，BL-SAM器件保持其初始性能的87%，而参比器件的效率降至63%和59%。

DoubleSAM2（PDF 第 10 页）

Original: Operational stability assessments were conducted using a multi-channel solar cell performance decay testing platform (PVLT-G8001M, Suzhou D&R Instruments Co. Ltd.) inside a nitrogen-filled glovebox, where the levels of H2O and O2 were maintained at approximately 100 ppm and 80 ppm, respectively. Devices were subjected to continuous illumination provided by a white LED light source (D&R Light, L-W5300KA-150, Suzhou D&R Instruments Co. Ltd.) simulating one sun intensity, with the initial JSC matching that under standard test conditions. Device performance was periodically tracked by I–V sweeps ranging from −1.35 to 0.2 V in 0.01 V increments. During the intervals between sweeps, an external load resistor-matched to the maximum power point (R = Imax / Vmax) was connected to ensure that the recorded PCE decay accurately reflected real-time performance degradation under simulated operating conditions. The MPP was automatically extracted based on the J–V data collected.

中文：运行稳定性评估使用多通道太阳能电池性能衰减测试平台（PVLT-G8001M，苏州德睿仪器有限公司）在氮气填充手套箱内进行，其中H2O和O2水平分别维持在约100 ppm和80 ppm。器件接受由白光LED光源（D&R Light, L-W5300KA-150，苏州德睿仪器有限公司）提供的模拟一个太阳光强的连续光照，其初始JSC与标准测试条件下的相匹配。器件性能通过−1.35至0.2 V、步进0.01 V的I–V扫描定期跟踪。在扫描间隔期间，连接与最大功率点匹配的外部负载电阻（R = Imax / Vmax），以确保记录的PCE衰减准确反映模拟运行条件下的实时性能退化。MPP根据收集的J–V数据自动提取。

DoubleSAM-SAME（PDF 第 8 页）

Original: We then tested the stability of devices with redeposited MeO-2PACz by subjecting encapsulated devices to ISOS-L-3 protocols (maximum power point tracking (MPPT) at 85 °C and 50% relative humidity (RH)), measuring their efficiency over time.

中文：随后，我们通过将封装器件置于ISOS-L-3协议下（在85 °C和50%相对湿度（RH）下进行最大功率点跟踪（MPPT）），并测量其效率随时间的变化，来测试使用重新沉积MeO-2PACz的器件的稳定性。

DoubleSAM-SAME（PDF 第 8 页）

Original: As shown in Figure 5c, control devices with unwashed MeO-2PACz rapidly degraded to 90% of their initial efficiency after 94 h. In contrast, devices with redeposited MeO-2PACz retained 90% of their initial efficiency after 480 h, a 5-fold improvement over the unwashed control device.

中文：如图5c所示，使用未清洗MeO-2PACz的对照器件在94小时后迅速衰减至初始效率的90%。相比之下，使用重新沉积MeO-2PACz的器件在480小时后仍保持初始效率的90%，相比未清洗对照器件提升了5倍。

DoubleSAM-SAME2（PDF 第 8 页）

Original: The PCE evolution of the unencapsulated WBG PSCs were monitored in accordance with the ISOS-L-1 test standard (Fig. 5i). D-2P-treated PSC still maintained more than 90% of its initial PCE after continuous 1-sun illumination conditions in nitrogen for 2500 h, while the S-2P-treated device has rapidly degraded to less than half its initial PCE after only 1000 h.

中文：未封装 WBG PSC 的 PCE 演化按照 ISOS-L-1 测试标准进行监测（图 5i）。D-2P 处理的 PSC 在氮气中连续 1 个太阳光照条件下 2500 h 后仍保持其初始 PCE 的 90% 以上，而 S-2P 处理的器件仅在 1000 h 后就迅速退化到其初始 PCE 的一半以下。

DoubleSAM-SAME2（PDF 第 9 页）

Original: Benefiting from improved electric field stability and light stability of perovskite film, the resulting PSC achieves improved long-term stability, and maintained more than 90% of its initial PCE after continuous 1-sun illumination conditions for 2500 h.

中文：得益于钙钛矿薄膜改善的电场稳定性和光稳定性，所得 PSC 实现了改善的长期稳定性，并在连续 1 个太阳光照条件下 2500 h 后保持其初始 PCE 的 90% 以上。